## Slide 1
The Goal:
Predict how long it takes an epoxy to cure at a given temperature.

## Slide 2
The Problem:
Can’t test it directly.

## Slide 3
The Problem:
In the process of heating the sample to the target temperature,
The cure advances at intermediate temperatures.

## Slide 4
The Solution:
“Isoconversional” techniques.

## Slide 5
Isoconversional:
The rate that the cure progresses depends only on:
The current temperature and
The current degree of cure
(0% - 100%)

## Slide 6
The Plan:
Heat the epoxy at a controlled temperature ramp.
Record the temperature and information about cure.

## Slide 7
The Data:
The following slides show pre-processing of the data.

## Slide 8
As the epoxy cures, it gives off heat.

## Slide 9
The blue hatched region is total amount of heat energy given off.

## Slide 10
At the time marked by the red arrow, 20% of the total heat energy has been given off.

## Slide 11
At the time marked by the purple arrow, 80% of the total heat energy has been given off.

## Slide 12
We define our degree of cure as the portion of heat given off.

## Slide 13
Repeating this study with various heating rates…

## Slide 14
…gives us a breadth of data to use for our predictions.

## Slide 15
The Math:
At the end of the day, we want the time it takes to reach a degree of cure.

## Slide 16
The Math:
(Please forgive the calculus)

## Slide 17
The Math:
Time to reach α
Isothermal temperature
For prediction
Temperature and time from experimental data
Gas constant
Something else altogether… we need to calculate this.

## Slide 18
The Math:
We’ll calculate Eα by minimizing this cost function. (Find the value of Eα for which φ has the lowest value.)

## Slide 19
Eα is out “Activation Energy”. It varies with degree of cure.

## Slide 20
Now we can predict cure time for any isothermal temperature!

## Slide 21
Validation:
…but is it right?

## Slide 22
This is data from the experimental runs.

## Slide 23
Now with predicted results on top.
It looks good!