## Slide 1
The Goal:
Predict how long it takes an epoxy to cure at a given temperature.

## Slide 2
The Problem:
Can’t test it directly.

## Slide 3
The Problem:
In the process of heating the sample to the target temperature,
The cure advances at intermediate temperatures.

## Slide 4
The Solution:
“Isoconversional” techniques.

## Slide 5
Isoconversional:
The rate that the cure progresses depends only on:
The current temperature and
The current degree of cure
(0% - 100%)

## Slide 6
The Plan:
Heat the epoxy at a controlled temperature ramp.
Record the temperature and information about cure.

## Slide 7
The Data:
The following slides show pre-processing of the data.

## Slide 8
As the epoxy cures, it gives off heat.

## Slide 9
The blue hatched region is total amount of heat energy given off.

## Slide 10
At the time marked by the red arrow, 20% of the total heat energy has been given off.

## Slide 11
At the time marked by the purple arrow, 80% of the total heat energy has been given off.

## Slide 12
We define our degree of cure as the portion of heat given off.

## Slide 13
Repeating this study with various heating rates…

## Slide 14
…gives us a breadth of data to use for our predictions.

## Slide 15
The Math: